## Slide 1: 18th Conference on Targets and Target Chemistry
Preliminary results of Zinc recycling for 68Gallium liquid target routine production
Antje Uhlending
Cyclotron Engineer
Department of Radiology, Nuclear medicine and Molecular Imaging

## Slide 2: 18th Conference on Targets and Target Chemistry
Content
1
68Ga radiotracer production from 68Ga liquid target
68Ga liquid target upgrade
Original post prosessing and the optimization of the purification process
Labeling and the fine tuning labeling
Requirements for recycling zinc solution
Recycling process
Results
Conclusion

## Slide 3: 18th Conference on Targets and Target Chemistry
68Ga radiotracer production from 68Ga liquid target
The first challenge for using recycled Zinc is the implementing of a
Stable
Flexible 68Ga-Radiotracer-routine production
Routine suitable
Cyclotron
68Zn (p.n) 68Ga
Purification
68Zn/68Ga
->
68Ga Cl3
Peptide Synthesis
  68Ga-PSMA
  68Ga-DOTATOC
2

## Slide 4
IBA Nirta Conical® C8 with 2.8 ml
Helium cooling upgrade 300 W (Alfa Laval)
Protection of the Helium cooling with stainless steel trap
Metal-free loading valve (Vici)
IBA 18/9 H03
Installation 1994
68Ga-irradiation parameter
Bam current 45 µA
Target pressure 8 – 20 bar
Irradiation time 30 – 50 min
Target foil 250 μm niobium
Target solution 68Zn(NO3)2 (99.5%)
Target concentration 33 – 66 mg/ml (0.5- 1.0 molar)
68Ga liquid target upgrade
18th Conference on Targets and Target Chemistry
3

## Slide 5
Original Post Processing
Post processing module: IBA Synthera® Extension
Chemicals: Fludomica®
SCX
SAX
Target
solution
Aceton/HBr
Zn2+
68Ga/68Zn in HNO3
[68Ga]Ga2Cl7-
0.1 mol/l HCL 68[Ga]GaCl3
18th Conference on Targets and Target Chemistry
4

## Slide 6
Optimization of the purification process
1. Optimizing Step:
SCX Chromafix® PS-H+
SAX Chromafix® HR-XA
2. Optimizing Step:
Additional washing SAX with 8M HCl
Zinc content after purification < 0.1 µg/ml Zinc
SCX
SAX
Target
solution
Aceton/HBr
Zn2+
[68Ga]Ga2Cl7-
Wasching with 8M HCl
 | Zinc Content [68Ga]GaCl3 [µg/ml]
Original Setting | 4.0
Cartridge Change | 2.1
Washing step of SAX | < 0.1
0.3 mol/l HCL 68[Ga]GaCl3
18th Conference on Targets and Target Chemistry
5

## Slide 7
Labeling module: Elysia Raytest®
Chemicals: ABX
68Ga-Peptide Labeling
6
18th Conference on Targets and Target Chemistry
80-950C
5-10 Min.
10 ml 0.3 mol/l HCl
[68Ga]GaCl3
C18
SCX
68Ga-Tracer
NH4OAc -Buffer

## Slide 8
Fine tuning 68Ga-Peptide labeling process
Variation | [68Ga]Ga-PSMA-11 | [68Ga]Ga-DOTA-TOC
Washing step: SCX with H2O | 50 ml | 50 ml
Buffer | 3.1 mL Acetate buffer | 3.0 ml HEPES buffer
Masking of Fe traces | 900 ng Ascorbic acid | 450 ng Ascorbic acid
Washing step: C18 with H2O | Not needed | 20 ml
7
18th Conference on Targets and Target Chemistry
80-950C
5-10 Min.
10 ml 0.3 mol/l HCl
[68Ga]GaCl3
C18
SCX
68Ga-Tracer
HEPES or NaOAC Buffer + Ascorbic acid
H2O
H2O
[68Ga]Ga-PSMA-11
[68Ga]DOTA-TOC

## Slide 9
18th Conference on Targets and Target Chemistry
8
Requirements for recycling zinc solution
The basic requirement is stable 68Ga-Radiotracer-routine production:
Using only ultra pure chemical quality and metal free items
Collecting only the 68Zn-target-solution
Residue
Aceton/HBr solution
Residue only
68Zn-target-solution
SCX
Target solution
2. Collected waste (Aceton/HBr)
50 ml
68Ga/68Zn in HNO3
Washing solution Aceton/HBr
1. Collected waste (Zn2+ in HNO3)
10 ml

## Slide 10
Recycling process
18th Conference on Targets and Target Chemistry
9
1.
Collect SAX waste
2.
Dissolve the residue Zinksalt in
3.
Precipitating
4.
Dissolve ZnS in cons. HCl and
5.
Dissolve ZnCl in
evaporate
(Zn2+ in HNO3) and evaporate till dry
2 mol/l HCl
0.2 mol/l HNO3
and sterile filtration
Zn2+ +
pH 8 -9 ZnS

## Slide 11
Results Recycling
18th Conference on Targets and Target Chemistry
10
Quality of [68Ga]GaCl3 after post processing:
Recycling yield of 68Zn:
Callculated 68Zn used for 60 runs with 45 mg/ml 2700 mg 68Zn
Amount of 68Zn in waste solution ( EDTA titrated) 2600 mg 68Zn
Amount of 68Zn in 68ZnS 2590 mg 68Zn
Amount of 68Zn in recycled target soultion 2585 mg 68Zn Recovery yield 95.7 %
Quality [68Ga]GaCl3 | Original [68Zn]Zn(NO3)2 | Recycled [68Zn]Zn(NO3)2
pH | 0.7 | 0.7
Zn | < 0.1 µg/ml | < 0.1 µg/ml
Fe | < 0.1 µg/ml | < 0.1 µg/ml
Endotoxin | < 0.25 EU/ml | < 0.25 EU/ml
67Ga (EOP) | 0.59 % | 0.48 %
67Ga (1h EOS) | 1.12 % | 0.87 %
67Ga (2h EOS) (< 2% Pharm. Eu) | 1.80 % | 1.35 %

## Slide 12
68Ga-Peptide labeling results
[68Ga]Ga-PSMA-11
[68Ga]DOTA-TOC
[68Ga]Ga-PSMA-11
[68Ga]DOTA-TOC
18th Conference on Targets and Target Chemistry
11

## Slide 13
Results
Since January 2021:
300 successful 68Ga-Radiotracer-production
100 successful 68Ga-Radiotracer-production with recycled Zinc solution
1.2 - 3.0 GBq (EOS) produced Activity of
[68Ga]Ga-PSMA-11
[68Ga]DOTA-TOC
Radiochemical purity
> 95% [68Ga]Ga-PSMA-11
> 90% [68Ga]DOTA-TOC
< 2 % free 68Ga
< 2 % 67Ga 2h EOS
18th Conference on Targets and Target Chemistry
12

## Slide 14
Conclusion
Implementing of a stable, routine suitable 68Ga-radiotracer routine production
Collecting only Zinc waste
Metal free process by using ultra pure chemical quality
Sufficient recovery yield
Equal quality of [68Ga]GaCl3 after purification
Good 68Ga-Peptide labeling results and quality
18th Conference on Targets and Target Chemistry
13
Checklist: Zinc recycling in 68Ga radiotracer production from 68Ga liquid target

## Slide 15
Heart and Diabetes Center
North Rhine-Westphalia
Bad Oeynhausen
Germany
Acknowledgements
IBA Ion Beam Applications
Fluidomica, target solutions
18th Conference on Targets and Target Chemistry
14

## Slide 16
18th Conference on Targets and Target Chemistry
any questions
?