## Slide 1
Development of Enriched Gadolinium Target for Cross Section Measurement and Future Production of Terbium
Yizheng Wang, Thomas Sounalet, Arnaud Guertin, Férid Haddad, Nathalie Michel, Etienne Nigron
18th Workshop on Targetry and Target Chemistry
AUGUST 22, 2022

## Slide 2
Terbium: a competitive candidate for theranostics
T1/2 = 4 h
Eα = 4 MeV, Eβ+ = 638 keV
Applied in “Alpha-PET”
(Muller, 2017; Umbricht 2019)
T1/2 = 7 d
Mean Eβ- = 154 keV
An alternative to 177Lu
Applied in β therapy
(Lehenberger, 2011; Gracheva, 2019)
T1/2 = 18 h
Mean Eβ+ = 1,14 MeV
Applied in PET/CT
(Muller, 2016; Baum 2017)
T1/2 = 5 j
Eγ= 87 MeV (32%)
EAuger= 87 keV (37%)
Applied in SPECT + Auger therapy
(Muller, 2014; Baum 2017)
Introduction
Cross section
Thick target
Conclusion Perspectives
Thin target
Mass production

## Slide 3


This work: produce 149,152,155 Tb with enriched Gd targets by cyclotrons
Produced by nuclear reactors: large quantity and good quality
  160Gd(n,γ)161Gd →161Tb
Produced by spallation reactions: limited quantity and complex procedure
  High energy (1,4 GeV) and many impurities
  Low efficiency to separate impurities
Lower energy (10-20 MeV), lower cost, less impurities
152Gd (p, 4n)149Tb (enrichment of 152Gd: 30%)
152Gd (p, n) 152Tb
155Gd (p, n) 155Tb, 155Gd (d, 2n) 155Tb (enrichment of 155Gd: 90%)

Production routes of Tb radionuclides
Introduction
Cross section
Thick target
Conclusion Perspectives
Thin target
Mass production

## Slide 4
Objectives : produce 155Tb using 155Gd
Introduction
Irradiation
Comptage
Résultat
Conclusion et Perspectives
Cible préparation
Introduction
Cross section
Thick target
Conclusion Perspectives
Thin target
Mass production
Cross section measurement of the reaction 155Gd(d,n)155Tb to estimate production yield
Make very thin targets (10-20 µm)
Manufacture a complete and uniform Gd-containing target for the routine production of Tb
Make thicker targets (≥ 100 µm)
1
2

## Slide 5
Objectives : produce 155Tb using enriched Gd
Introduction
Irradiation
Comptage
Résultat
Conclusion et Perspectives
Cible préparation
Prepared enriched Gd2O3 (Trace Science):
Isotopes | Gd-155 | Gd-156 | Gd-157 | Gd-158 | Gd-160
Proportion (%) | 92.8 | 5.7 | 0.8 | 0.5 | 0.2
σ maximum produced by proton: 400 mb
σ maximum produced by deuteron: 1000 mb
Introduction
Cross section
Thick target
Conclusion Perspectives
Thin target
Mass production

## Slide 6: Thin targets fabrication: Co-electrodeposition method
The reduction potential of Gd3+/Gd is too negative (-2,3 V/ENH) to obtain an adhered deposit in aqueous solutions because of the HER.
WHY?
Insoluble Gd2O3 particles are mixed in the alkaline Ni plating bath, by applying a potential, the Gd2O3 particles will move with Ni2+ and trapped in the Ni metal matrix (mechanical process).
HOW?
A Ni-Gd2O3 composite target with a thickness of 10-20 µm can be obtained.
WHAT?
Introduction
Cross section
Thick target
Conclusion Perspectives
Thin target
Mass production

## Slide 7
Obtained targets: thin and homogenous
One hour of co-electrodeposition
Au substrate
Thickness = 13 µm
Gd trapped in the deposit: 3 mg
Morphological analysis: SEM
E = 15kV, magnitude x100
Mesure time = 60 s
E= 15kV, zoom x1000
Composition analysis: EDX et ICP-OES
According to the ICP-OES results, the target contains about 3 mg of Gd atoms.
Introduction
Cross section
Thick target
Conclusion Perspectives
Thin target
Mass production
For 1 g of Gd2O3 powder, 10 targets was made, 0.6 g of powder left.

## Slide 8: Cross section measurement: stacked-foils technique
Schematic diagram of the stack composition
Target: Ni/Gd2O3 composite target deposited on the Au substrate
Monitor: Ti and Ni foils (measure 48V and 58Co)
Degrador: Al foils
Beam line used at ARRONAX cyclotron facility
Introduction
Cross section
Thick target
Conclusion Perspectives
Thin target
Mass production

## Slide 9: Reliability of obtained targets?
Eight targets made with natural Gd2O3 powder were used to measure the σ of natGd(d,x)155Tb:
The measured results are consistent with existing data.
Introduction
Cross section
Thick target
Conclusion Perspectives
Thin target
Mass production

## Slide 10: Cross sections measured for 155Tb
The contribution of 156Gd starts when energy is bigger than 13 MeV.
We got 4 measured cross section values of the reaction 155Gd(d,2n)155Tb.
Introduction
Cross section
Thick target
Conclusion Perspectives
Thin target
Mass production

## Slide 11: Cross sections measured for 153,154,156Tb
156Tb always exits while 153Tb and 154Tb can be limited by limiting energy.
Introduction
Cross section
Thick target
Conclusion Perspectives
Thin target
Mass production

## Slide 12: Estimation of production yield
Introduction
Cross section
Thick target
Conclusion Perspectives
Thin target
Mass production
The purity of 155Tb varies from 60% to 89% when energy varies from 9 to 15 MeV.

## Slide 13: Thick targets fabrication: pelletizing method
Introduction
Cross section
Thick target
Conclusion Perspectives
Thin target
Mass production
Mass = 0.6 g, thickness = 0.4 mm

## Slide 14: First test of mass production
Production yield:
Tb-155: 10.2 ± 0.7 MBq/µAh
Tb-156: 1.3 ± 0.1 MBq/µAh
Introduction
Cross section
Thick target
Conclusion Perspectives
Thin target
Mass production
Estimation according to the measured excitation function:
Experiment:
Eincident = 15.1 MeV, Eoutgoing = 8.6 MeV
500 nA for 1 h
Purity of Tb-155: 89% (10 d after EOB)

## Slide 15: Conclusion and perspectives
Work completed:
Cross section measurement:
The cross sections of *Gd(d,x)155Tb and other impurities have been measured using Ni-Gd2O3 composite targets.
First test for mass production:
Production yield Tb-155 is about 10 MBq/µAh, purity is about 89%.
Follow-up:
Modification of encapsulation system.
Purification
Introduction
Cross section
Thick target
Conclusion Perspectives
Thin target
Mass production

## Slide 16: Thank you for your attention!
If you have any questions, please contact: yizheng.wang@subatech.in2p3.fr