## Slide 1
Production of 55Co Using Pressed Nickel and Magnesium Foils
Jonathan Siikanen1.3, Stefan Milton2,3, Mélodie Ferrat2,3, Erik Samén2,3, Emma Jussing2,3, Thuy. A. Tran2,3
1Karolinska University Hospital, Department of Medical Radiation Physics and Nuclear
Medicine, Stockholm, SWEDEN, 2Karolinska University Hospital, Department of
Radiopharmacy, Stockholm, SWEDEN, 3Karolinska Institutet, Department of Oncology and Pathology, Stockholm, Sweden

## Slide 2: Overview
Introduction of 55Co
Motivation for pressed Ni/Mg powder
Making targets
Target performance
Conclusions
Acknowledgements

## Slide 3: 55Co
Production on PET-cyclotrons
  54Fe(d,n) 55Co (Naturally: 6 % 54Fe)
  58Ni(p,α)55Co (Naturally: 70 % 58Ni)
Known chemistry
  AG1-X8, DGA, etc.
  DOTA, NOTA, etc.
β+ =76 %, EK=0.4-0.6 MeV

## Slide 4: 55Co for PET: Different molecules require different radionuclides
T1/2 (h)
89Zr 74
55Co 18
64Cu 13
58mCo 9
66Ga 9
45Ti 3
61Cu 3
68Ga 1
Theranostic pair with 58mCo

## Slide 5: Motivation for pressed Ni/Mg powder
Speeds up dissolution
  (with heating: plated =0.5-1h, intact foils= hours)
Mg dissolves fast in HCl
  Creates spongy Ni-matrix with increased surface area
Also:
Making mechanically stable foils from metal powder
Fast and easy to produce
“sponge effect”

## Slide 6: Motivation for pressed Ni/Mg powder
Distribution coefficient of Mg is very low for AG1-X8 in strong (6-10 M) HCl (Kraus and Nelson 1958)
Thermal conductivity (W·m−1·K−1)
  Mg= 156, Ni=98
Irradiation of Mg
  13 MeV P, 4 h 102 Bq 22Na (T1/2=2.6 y) and short lived (sec) Al isotopes
https://www-nds.iaea.org/relnsd/isotopia/isotopia.html

## Slide 7: Pressing natNi/Mg-foils in 5 min
350 USD
400 USD
20 ton, 1.1 GPa
15 mm d
Mg
Ni

## Slide 8: natNi/Mg-foils
Thickness (mm): 0.2 0.4 0.8
Diameter = 15 mm
Thickness = 0.3 mm

## Slide 9: natNi and Mg
pressed natNi (150 mg)-Mg (50 mg) foil
b) a natNi (200 mg) foil.
The 100% natNi foils were fragile containing cracks and were not suited for bombardment because the risk of foil fragmentation inside the solid target system.

## Slide 10: Making 58Ni/Mg-foils (58Ni 2000 EUR/g or 300 EUR/foil)
Mg
natNi
58Ni
+
or
<50 µm
Up to 3 mm
Mg: 50 mg
Ni: 150 mg

## Slide 11
PETtrace, GE Healthcare
  Ep ~16 MeV
  Ip=130 µA
Comecer ALCEO EDS/PTS
  Ep degraded to ~12.6 MeV
    500 µm Al-foil
  Ip= 25 µA
Cyclotron & Solid Target System

## Slide 12: Enriched 58Ni (Metal Powder)
Isotope | 58Ni | 60Ni | 61Ni | 62Ni | 64Ni
Enrichment (%) | 99.905 | 0.083 | 0.004 | 0.004 | 0.004
Chemical admixture |  |  |  |  | 
Element | Al | Co | Cr | Cu | Fe
Content (ppm) | < 10 | < 10 | < 10 | <10 | <10
Element | Mg | Mn | Pb | Si | Ti
Content (ppm) | <10 | 10 | <10 | <10 | <10
Element | Zn | C | S | P | 
Content (ppm) | <10 | 104 | <10 | 2 | 
Threshold
58Ni(p,2p)57Co 8.3 MeV
60Ni(p,α)57Co 0.3 MeV
Notes: 58Ni only as powder

## Slide 13
Ein=12.6 MeV
Eexit= 6 MeV
0.3 mm
150 mg Ni
50 mg Mg
58Ni(p,α)55Co
58Ni(p,x)57Co
Reimer & Qaim 1997
IAEA NDS

## Slide 14: Irradiations
10, 18, 25 µA
1-180 min
Completely intact without burn marks
25 µA, 3 h

## Slide 15
AG1-X8 resin (2g)
Pre cond: 10 ml 9.5 M HCl
4 ml 9.5 M HCl + 0.4 ml HNO3 (70%)
4 min waiting
1 ml H2O + 0.4 ml H2O2 (70%)
5 ml 9.5 M HCl
Dissolution in 50 ml falcon tube
Wash: 30 ml 9.5 M HCL
Elution: 4 ml, 0.25 M, HEPES
Wash waste: Remaining 58Ni/Mg + trace metals
Waste:58Ni/Mg target material
Elution: cobalt in HEPES
Frit filter
Purification
Notes: We are using a higly oxidative and strong acid solution to dissolve our foils

## Slide 16: Dissolution & Purification
Automated with Comecer Taddeo PRF
Ultra pure water, chemicals and no metal needles etc.
Dissolution (without heating)=10 min
  Pressed Ni > 1h
  Ni-foil > many hours
Purification=20 min
Total= 35 min
  Including shuttle drying=5 min

## Slide 17: Production and QC
Produced activity & Half-life: Capintec Dose Calibrators
RNP: Energy & Efficiency calibrated HPGE-detector (Canberra)
  2 and 17 h post EOB
Ni breakthrough assessed with semi-quantitative test strips (Quantofix)
Apparent Molar Activity (AMA): DOTA-titration in 0.25 M HEPES adjusted to pH 7.0
Notes: using NaOH. TLC (0.5 M triethylammonium acetate in acetonitrile:H2O 1:1, SG 60 RP-18 (F254S) TLC-strip)

## Slide 18
Results |  | comment
Produced A in foil | 340±10 MBq (EOB) | A_sat=120±5 MBq/µA
55Co at EOP (35 min post EOB) | 240±20 MBq 60 MBq/ml HEPES | 5 min shuttle drying 10 min dissolution 20 min purification
Isolated 55Co/Foil 55Co (EOP) | >70 % | Un-dissolved larger grains
RCY (EOP) | 82±2 % | Y=prod/(waste+resins+prod)
Ni in eluate | 0 mg/L | Semi-quantitative Strips
AMA at EOB | 1.8±0.2 GBq/µmol DOTA | (3.6 GBq/µmol x 50 %)
RNP (EOB) | 99.98±0.014 % | 2h & 17 h post EOB Contaminant is 57Co
T1/2 | 17.48 h | 17.53 h (Nudat3)
pH | ≤1 | 

## Slide 19: Conclusions
Easy to make mechanically stable foils from commercially available 58Ni-powder
Mixed Ni/Mg foils dissolves rapidly due to “Sponge effect” at room temperature
Foils looked completely intact after long irradiations with 25 µA
  Should tolerate more beam, 50, 100, 150 µA?
Mg does not seem to disturb purification and chelation chemistry for a “standard” Ag1-X8 resin

## Slide 20
Thuy Tran, Associate professor, Team leader
Emma Jussing, PhD, Researcher
Stefan Milton, PhD, Researcher
Mohammad Moein, PhD, Researcher
Erik Samén, PhD, Researcher
Melodie Ferrat, PhD, Post doc
Ida Friberger, PhD student
+ more students starting..
Acknowledgements to research team Thuy Tran