## Slide 1
Possible Material-Saving Approach of Sputtering Techniques for Radiopharmaceutical Target Production
Ph.D student
Alisa Kotliarenko
Co-authors: Dr. Oscar Azzolini, Sara Cisternino, Mourad El Idrissi, Dr. Giorgio Keppel , Dr. Juan Esposito
18th Workshop on Targetry and Target Chemistry Whistler, BC August 22-26, 2022

## Slide 2: Work Goal
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
2/21
This research was funded by CSN5 of the INFN, Italy for 2018–2022, in the framework of METRICS project. PI: J. Esposito
and by INTEFF program at INFN funded by MISE, Italy – in the framework of TOTEM project PI: S.Cisternino.
To evaluate the main magnetron sputtering technique issues and to found a possible solution to use this technique for solid target production

## Slide 3: Outline
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
3/21
Introduction to Sputtering techniques
Results on magnetron sputtering optimization
Results on nat-ZnO targets realization
1
2
3

## Slide 4: Surface Technologies and Superconductivity Service
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
Chemistry laboratory
Cryo laboratory
Sputtering laboratory
Advanced surface treatments for Cu and Nb accelerating cavities
Superconductive Nb depositions
Cryogenic characterization
Various PVD machines for industrial and scientific interests
Deposition of metals and ceramic compounds on different substrates
4/21
1

## Slide 5: Magnetron sputtering
5/21
Planar magnetron sputtering
1
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it

## Slide 6: Magnetron sputtering
5/21
Idea of inverted magnetron sputtering
1
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
Planar magnetron sputtering

## Slide 7: Magnetron sputtering - characteristics
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
Material sputtered everywhere in the vacuum chamber
Material losses – 80%
6/21
Precise thickness control
High adherence
Densification of the deposition
1

## Slide 8: Magnetron sputtering for target production
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
nat-Mo targets preparation
[Skliarova et al., Molecules 2021]
nat-Y target preparation
7 targets simultaneous depositions
Thickness range – 150-200 µm
7/21
1
[Patent n. WO 2019/053570]

## Slide 9: Possible material-saving approach
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
8/21
2 inch planar magnetron evaluation
Recovering shield
Magnetron and diode sputtering techniques
2
Notes: Idea of the reaserch ( article)
The combination of MS and DS

## Slide 10: Possible material-saving approach
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
9/21
[Kotliarenko et al., Applied Science 2021]
Material results | Magnetron,% | Diode, %
On the substrate | 38,9±0,003 | 21,6±0,035
On the shield | 56,3±0,005 | 71,6±0,113
Losses | 4,8±0,008 | 6,8±0,148
Growing beheviour of MS and Diode depositions
2
Notes: Idea of the reaserch ( article)
The combination of MS and DS

## Slide 11: Inverted magnetron idea
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
Simpler system
Does not require shielding
Easy maintenance
Ground shield
Cathode
Cathode
10/21
Produced prototype
2
Initial design
Prototype design
Dimensions:
External h 106 mm Ø 89 mm
Cathode h 106 mm Ø 59 mm
Dimensions:
External h 80 mm Ø 160 mm
Cathode h 60 mm Ø 100 mm

## Slide 12: Inverted magnetron - proof of concept
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
Deposition parameters
Cu deposition: Ø10 mm x 40 µm
Nb: Ø24 x 0,5 mm
Morphology of Cu deposition
11/21
TEST 30
Gas flows: Ar – 3,5 sccm
Power: Iconst 1 A;
U 500 V
Time: 150 min
Coil power: 5,5 A
2

## Slide 13: Inverted magnetron – standart magnetron
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
12/21
Growing beheviour of Cu deposition
Inverted MS
Standard MS
2

## Slide 14: nat-ZnO deposition test
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
Zn cathode
Reactive gas – O2
Reactive process of ZnO
Reactive sputtering process
13/21
3

## Slide 15: nat-ZnO deposition test - results
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
Gas flows: Ar - 4 sccm
O2 - 2 sccm
Power: Iconst 0,7 A;
U 450 V
Time: 115 min
Coil power: 6 A
TEST ZnO - 8
Morphology of ZnO deposition
14/21
3

## Slide 16
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
Polycristalline growing beheviour of ZnO deposition
15/21
3
Deposition rate: 130 nm/min
Gas flows: Ar - 4 sccm
O2 - 2 sccm
Power: Iconst 0,7 A;
U 450 V
Time: 115 min
Coil power: 6 A
nat-ZnO deposition test - results
TEST ZnO - 8

## Slide 17
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
nat-ZnO deposition test - results
Interface analysis
High adhesion of ZnO to Nb
16/21
Sample preparation
Cutting with electro erosion and step-lapping with different abrasive papers
3

## Slide 18
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
nat-ZnO deposition test - results
XRD diffractogram
Crystalline structure
Similar to nat-ZnO powder
Preferential (002) crystal growing
17/21
3

## Slide 19
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
nat-ZnO deposition test - results
20 µm
Sputtering parameters
Gas flows: Ar - 4 sccm
O2 - 2 sccm
Power: Iconst 0,7 A;
U 450 V
Time: 130 min
Coil power: 6 A
Gas flows: Ar - 4 sccm
O2 - 2 sccm
Power: Iconst 0,7 A;
U 500 V
Time: 150 min
Coil power: 6 A
18/21
30 µm
3
Thickness uniformity measurements by profilometer
Deposited area - Ø10 mm

## Slide 20
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
nat-ZnO deposition test - results
Targets parameter
Morphology of ZnO targets
19/21
3
ZnO deposition:
Ø10 mm x 20 µm;
ρZnO~ 73 % bulk
Nb: Ø23.7 x 1,2 mm
Areal ρ ~ 8,4 mg/cm2
ZnO deposition:
Ø10 mm x 30 µm;
ρZnO~ 71 % bulk
Nb: Ø23.7 x 1,2 mm
Areal ρ ~ 12,1 mg/cm2

## Slide 21
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
nat-ZnO deposition test – irradiation
Energy 19 MeV,
p+ current 10 µA
5 min
Energy 19 MeV,
p+ current 20 µA
5 min
Irradiation parameter
Thermo-mechanical irradiations tests
20/21
3
ZnO deposition:
Ø10 mm x 20 µm;
ρZnO~ 73 % bulk
Nb: Ø23.7 x 1,2 mm
Areal ρ ~ 8,4 mg/cm2
ZnO deposition:
Ø10 mm x 30 µm;
ρZnO~ 71 % bulk
Nb: Ø23.7 x 1,2 mm
Areal ρ ~ 12,1 mg/cm2
Targets parameter

## Slide 22: Conclusions
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
Thank you for your attention!
Oscar Azzolini
Sara Cisternino
Surface Technologies and Superconductivity Service group
Mourad El Idrissi
1
Evaluation of sputtering techniques from the material point of view
Realization of recovering shield for standard magnetron deposition
An alternative sputtering configuration proposed and realized
First nat-ZnO targets realization by inverted magnetron technique
Is the magnetron sputtering technique suitable for ZnO target production?

## Slide 23: Conclusions
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
Thank you for your attention!
Oscar Azzolini
Sara Cisternino
Surface Technologies and Superconductivity Service group
Mourad El Idrissi
1
Evaluation of sputtering techniques from the material point of view
Realization of recovering shield for standard magnetron deposition
An alternative sputtering configuration proposed and realized
First nat-ZnO targets realization by inverted magnetron technique
Is the magnetron sputtering technique suitable for ZnO target production?

## Slide 24: Known hallow magnetron configuration
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
[O'Leary, Colm (1999) Design, construction and characterisation of a variable balance magnetron sputtering system. Master of Engineering thesis, Dublin City University.]

## Slide 25: Known hallow magnetron configuration
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
[J.B.K. Kana et al. / Applied Surface Science 254 (2008) 3959–3963]

## Slide 26: Work in consideration
cooling
COIL
COIL
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
Substrate
Nb backing
Mask
Mask
cooling
Reduced dimensions
Two targets deposition

## Slide 27: Work in consideration
cooling
cooling
COIL
Substrate
Nb backing
Mask
Mask
Sample holder
+ Mask
COIL
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it

## Slide 28
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it
Target preparation method | MS | HIVIPP | SPS
Target thickness | 0.1µm-1mm | 0.1-10µm | >150µm
Density, % of bulk | >95% | <80% | ~95%
Efficiency (reverse to material losses), % | <20% | 95% | >95%
Backing | Any | El. conductive | Metal
Target preparation time | 1-2 days | 1-2 days | minutes
Thermomechanical performance | >1kW/cm2 Excellent | Tested only at low current | >1kW/cm2 Excellent
Main defect | High losses | Thickness limitation | NO low thickness
Manufacturing techniques comparison

## Slide 29: XRD comparison
18th Workshop on Targetry and Target Chemistry Whistler
Alisa Kotliarenko – alisa.kotliarenko@lnl.infn.it

## Slide 30
Substrate
Mask
Mask
Nb backing
Permanent magnet
Cathode
Substrate
Nb backing
Mask
Mask
cooling
cooling
cooling
COIL
COIL