## Slide 1: An Aluminum-Indium-Silver Sealed Solid Cyclotron Target for High Yield Radiometal Production
Bryce Nelson, John Wilson, Jan Andersson, Frank Wuest
Department of Oncology
University of Alberta, Edmonton, Alberta, Canada

## Slide 2: Disclosures
A patent application has been filed for the described cyclotron target technology
Notes: Here are my disclosures

## Slide 3: Challenges with Existing Solid Targetry
Existing unsealed solid targets face several challenges
Risk of target material delamination and contamination during irradiation or upon download
Target material limited to compounds that can adhere to the target backing
Need an alternative target that can encapsulate a variety of sensitive or hazardous target materials and is conducive with post-irradiation processing (start with the chemistry, work back to the targetry)
?

## Slide 4
Image credit of Advanced Cyclotron Systems Inc. (ACSI)
TA-1186/TA-2150-B solid target assemblies (ACSI)
24 MeV TR24 Cyclotron (ACSI)
4 beamlines

## Slide 5
Pressed target material pellet placed in machined depression
Aluminum cover pressed onto indium wire encapsulates target material for bombardment, tab facilitates easy peeling removal
Improved heat transfer via target material contact with both Al cover and backing
Complete assembly
Aluminum cover
Indium wire
Machined aluminum or silver disc
Aluminum cover
Target material pellet
Aluminum or silver disc with machined depression
Indium wire
1 cm
Target pellet added to depression
Cyclotron Targetry

## Slide 6: Cyclotron Targetry
Fast to assemble, easy to handle, storable, contains reusable Al/In components
Flexible processing: Al disc resistant to HNO3, Ag disc resistant to HCl
Minimal activation with high purity Al disc (99.999%) permitting rapid reuse
Adaptable with a variety of target materials to produce other radionuclides

## Slide 7: 133/135La Theranostics
135La: Auger-Meitner electron therapy
133La: PET imaging
Modified from Darryl J Bornhop
Image from Helge Thisgaard
133/135La theranostic pair
Nelson et al., Sci Rep. 2020; 10(1)
Nelson et al., J Nucl Med. 2022;63(4):584-590

## Slide 8: Cross Sections Weighted for natBa Isotopic Abundance
Cross Section simulation data from TENDL 2019 (Koning et al.)
Chart: Beam Energy (MeV)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 22 | 24 | 26 | 28 | 30
Ba-137(p,3n)La-135 | 0 | 27.9328 | 151.264 | 539.939 | 830.191 | 965.682 | 1012.34 | 953.684
Ba-136(p,2n)La-135 | 0 | 198.114 | 517.036 | 728.438 | 868.208 | 959.632 | 1024.36 | 1070.73 | 1102.82 | 1121.03 | 1067.61 | 704.622 | 386.405 | 233.284 | 173.015
Ba-135(p,n)La-135 | 0 | 0.016285 | 0.67995 | 6.9167 | 31.9207 | 91.7416 | 195.84 | 337.521 | 491.005 | 630.964 | 686.236 | 474.158 | 276.582 | 165.71 | 114.242 | 88.92 | 77.2231 | 71.0991 | 67.3963 | 62.3659 | 58.1005 | 54.7286 | 51.5564 | 48.2669
Ba-135(p,3n)La-133 | 0 | 12.0667 | 272.727 | 625.675 | 842.071 | 932.306 | 951.592
Ba-134(p,2n)La-133 | 0 | 136.13 | 455.574 | 721.444 | 863.36 | 954.398 | 1015.51 | 1055.92 | 1080.05 | 1099.31 | 982.423 | 624.935 | 351.802 | 220.424
Ba-134(p,3n)La-132 | 0 | 124.503 | 489.678 | 762.87 | 879.194
Ba-132(p,n)La-132 | 0 | 24.2579 | 84.891 | 180.423 | 307.806 | 450.18 | 586.039 | 703.713 | 798.805 | 803.312 | 542.894 | 311.461 | 192.999 | 132.451 | 102.019 | 85.6718 | 69.9828 | 62.4871 | 57.6219 | 53.8295 | 50.2382
11.9 MeV | 0 | 850 | 1200
22 MeV | 0 | 850 | 1200
Chart: Beam energy (MeV)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 22 | 24 | 26 | 28 | 30
Ba-137(p,3n)La-135 | 0 | 3.1369 | 16.9869 | 60.6351 | 93.2304 | 108.4461 | 113.6858 | 107.0987
Ba-136(p,2n)La-135 | 0 | 15.5519 | 40.5873 | 57.1824 | 68.1543 | 75.3311 | 80.4123 | 84.0523 | 86.5714 | 88.0009 | 83.8074 | 55.3128 | 30.3328 | 18.3128 | 13.5817
Ba-135(p,n)La-135 | 0 | 0.0010732 | 0.044809 | 0.45581 | 2.1036 | 6.0458 | 12.9059 | 22.2426 | 32.3572 | 41.5805 | 45.223 | 31.247 | 18.2268 | 10.9203 | 7.5285 | 5.8598 | 5.089 | 4.6854 | 4.4414 | 4.1099 | 3.8288 | 3.6066 | 3.3976 | 3.1808
Ba-135(p,3n)La-133 | 0 | 0.7952 | 17.9727 | 41.232 | 55.4925 | 61.439 | 62.7099
Ba-134(p,2n)La-133 | 0 | 3.2943 | 11.0249 | 17.4589 | 20.8933 | 23.0964 | 24.5753 | 25.5533 | 26.1372 | 26.6033 | 23.7746 | 15.1234 | 8.5136 | 5.3343
Ba-134(p,3n)La-132 | 0 | 3.013 | 11.8502 | 18.4615 | 21.2765
Ba-132(p,n)La-132 | 0 | 0.024258 | 0.084891 | 0.18042 | 0.30781 | 0.45018 | 0.58604 | 0.70371 | 0.7988 | 0.80331 | 0.54289 | 0.31146 | 0.193 | 0.13245 | 0.10202 | 0.085672 | 0.069983 | 0.062487 | 0.057622 | 0.05383 | 0.050238
11.9 MeV | 0 | 850 | 1200
22 MeV | 0 | 850 | 1200
11.9 MeV
22 MeV

## Slide 9: Cyclotron Irradiation – natBa metal Target Material
200 mg natBa metal target material
Ag target backing
22 MeV for 133/135La production
11.9 MeV for 132/135La production
250 μm Ag foil degrader for 11.9 MeV
20 μA, 25 min (500 μA·min)
Beam energy (MeV) | 132La EOB yield (MBq) | 133La EOB yield (MBq) | 135La EOB yield (MBq)
11.9 | 0.82 | - | 17.9
22 | 0.38 | 231 | 166

## Slide 10: Cross Sections of Interest – Enriched 135BaCO3 Target Material
Cross section simulation data from TENDL 2019 (Koning et al.)
Chart: Beam energy (MeV)
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 22 | 24 | 26 | 28 | 30
Ba-137(p,3n)La-135 | 0 | 0.22346 | 1.2101 | 4.3197 | 6.6423 | 7.7255 | 8.0987 | 7.6295
Ba-136(p,2n)La-135 | 0 | 7.1718 | 18.7176 | 26.3727 | 31.4362 | 34.7497 | 37.0963 | 38.7782 | 39.9424 | 40.6034 | 38.6732 | 25.5359 | 13.9879 | 8.4449 | 6.2631
Ba-135(p,n)La-135 | 0 | 0.015125 | 0.63316 | 6.4626 | 29.8731 | 85.852 | 183.0445 | 314.9483 | 457.5246 | 587.3361 | 638.5167 | 441.8091 | 258.4847 | 155.5135 | 107.6368 | 84.056 | 73.1578 | 67.4672 | 64.0185 | 59.3575 | 55.3781 | 50.7334 | 47.7928 | 44.7434
Ba-135(p,3n)La-133 | 0 | 11.186 | 252.8272 | 580.0508 | 780.5998 | 864.2477 | 882.1258
Ba-134(p,2n)La-133 | 0 | 0.35394 | 1.1845 | 1.876 | 2.2453 | 2.4823 | 2.6416 | 2.7469 | 2.8099 | 2.8603 | 2.5566 | 1.6248 | 0.91469 | 0.5731
Ba-134(p,3n)La-132 | 0 | 0.32371 | 1.2732 | 1.9835 | 2.2859
Ba-132(p,n)La-132 | 0 | 0.012133 | 0.042651 | 0.091054 | 0.15564 | 0.2273 | 0.29536 | 0.35412 | 0.40151 | 0.40357 | 0.27318 | 0.15726 | 0.097846 | 0.067396 | 0.052041 | 0.043784 | 0.0359 | 0.03215 | 0.028811 | 0.026915 | 0.025119
11.9 MeV | 0 | 700 | 900
22 MeV | 0 | 700 | 900
24 MeV | 0 | 400 | 900

## Slide 11: Cyclotron Irradiation – BaCO3 Target Material
135BaCO3 (92.7%) and natBaCO3 target materials
Al target backing
23.3 MeV to maximize 133La production
11.9 MeV for 135La production, target installed in reverse with 1 mm Al disc acting as degrader
Direct water cooling on target back
10 μA, 10 min (100 μA·min)
Beam Energy (MeV) | 135BaCO3 target activity of La isotopes (MBq) |  | natBaCO3 target activity of La isotopes (MBq) | 
 | 135La | 133La | 135La | 133La
11.9 | 81 ± 2 | 0 | 6.8 ± 0.4 | 0
23.3 | 28 ± 1 | 214 ± 7 | 35 ± 1 | 59 ± 2
23.3 MeV energy irradiation
11.9 MeV energy irradiation
Proton beam
Al cover
Al disc

## Slide 12: Derenzo Phantom PET Imaging - Spatial Resolution
PET radionuclides in order of increasing positron Emean and Emax
18F, 64Cu, 44Sc and 68Ga from Ferguson et al., EJNMMI Phys. 2019; 6(1)
Derenzo phantom assembly for investigating PET spatial resolution
Nelson et al., J Nucl Med. 2022;63(4):584-590
Notes: And there is a strong correlation between the radionuclide positron energy and spatial resolution. Comparing to PET phantom data for fluorine, copper, scandium, and gallium from a recent paper by Ferguson et al, Lanthanum 133 clearly exhibits superior spatial resolution to scandium 44, the widely used radiometal gallium 68, and another radiolanthanum PET candidate, lanthanum 132, and looks decent even compared to the PET imaging spatial resolution gold standards F-18 and Cu-64. This highlights the excellent image quality obtainable from lanthanum 133.

## Slide 13: Radiolabeling
Radiolabeling performed with DOTA and Macropa
Use [133La]LaCl3 produced with isotopically enriched 135BaCO3 target material, Ba/La separation performed using branched DGA resin
Adjust [133La]LaCl3 to pH 4.5 with NaOAc buffer
DOTA: React at 90°C for 30 min
130 ± 15 GBq/μmol (133La)
Macropa: React at 22°C for 10 min
206 ± 31 GBq/μmol (133La)
DOTA
Macropa
133La
133La
Nelson et al., J Nucl Med. 2022;63(4):584-590
Separation modified from Aluicio-Sarduy et al., Sci Rep. 2019; 9(1)
Notes: After separation is complete, we used 100 microliter aliquots our lanthanum-133 to radiolabel the chelators DOTA and macropa.
To radiolabel DOTA and macropa, we first adjust to pH 4.5 with sodium acetate buffer.
Then, we react at 90oC for 30 mins for DOTA, and room temperature for 10 min with macropa.
We achieved full incorporation, and 130 GBq/umol with DOTA, and 206 GBq/umol with macropa.

## Slide 14: Preclinical PET Prostate Cancer Imaging
PET imaging of LNCaP tumor-bearing male NU/NU mice injected with [133La]La-PSMA I&T and DCFPyL
Nelson et al., J Nucl Med. 2022;63(4):584-590
Notes: Upon injection in the mouse, the lanthanum-133 radiopharmaceutical was allowed to accumulate for 60 min prior to PET imaging, and as you can see in the left image, the LNCaP tumor is clearly visualized with high spatial resolution, with a high SUV value, which measures radiotracer uptake.
Next, for a blocking experiment, we used the PSMA targeting agent DCFPyL. As PSMA I&T and DCFPyL contain the same PSMA targeting motifs and have similar IC50 values with LNCaP cells, DCFPyL should serve as an effective competitive inhibitor to try to prevent our lanthanum-133 PSMA I&T from binding to the tumor. And as you can see in the right image, mice predosed with DCFPyL exhibited significant tumor blocking of lanthanum-133PSMA I&T, with the tumor PET signal vanishing. The graph on the right shows the quantification of this consistent blocking effect. This demonstrated the high affinity of the lanthanum-133 PSMA I&T for the LNCaP cells.
All of this data for our improved targetry, chemical separation, phantom and animal imaging was published in a recent article in the Journal of Nuclear Medicine.

## Slide 15: 64Cu Production Cross Sections of Interest – Enriched 68Zn Target Material
Cross section simulation data from TENDL 2019 (Koning et al.)

## Slide 16: Cyclotron Irradiation
100 mg 68Zn (98.3%) sandwiched between two 0.075 mm graphite foils
24 MeV (extracted), 23 MeV incident on 68Zn at currents up to 70 μA
Ag foil behind target disc backing with direct water cooling in TA-1186 (exit beam energy <7 MeV to stop water activation), helium cooling on target front
64Cu saturated yield of 348 ± 6 MBq/μA (n=3)
Complete assembly
Top graphite foil
68Zn pellet on graphite foil
Machined aluminum disc
Base graphite foil in depression

## Slide 17: 64Cu Purification and Radiolabeling
Co-produced 67Cu (<0.3% at EOB), large 67/68Ga activities
64Cu purified using a CU/TBP/TK201 resin combination
>94% 64Cu decay-corrected yield in <2 mL [64Cu]CuCl2
Besides 67Cu, no detectable radionuclidic impurities
Full radiolabeling incorporation down to 1 μg with DOTA, NOTA, TETA chelators
HPGe gamma emission spectrum of [64Cu]CuCl2 product

## Slide 18: Preclinical PET Prostate Cancer Imaging
Preclinical PET imaging of LNCaP tumor-bearing male NU/NU mice injected with [64Cu]Cu-PSMA I&T
Notes: Upon injection in the mouse, the lanthanum-133 radiopharmaceutical was allowed to accumulate for 60 min prior to PET imaging, and as you can see in the left image, the LNCaP tumor is clearly visualized with high spatial resolution, with a high SUV value, which measures radiotracer uptake.
Next, for a blocking experiment, we used the PSMA targeting agent DCFPyL. As PSMA I&T and DCFPyL contain the same PSMA targeting motifs and have similar IC50 values with LNCaP cells, DCFPyL should serve as an effective competitive inhibitor to try to prevent our lanthanum-133 PSMA I&T from binding to the tumor. And as you can see in the right image, mice predosed with DCFPyL exhibited significant tumor blocking of lanthanum-133PSMA I&T, with the tumor PET signal vanishing. The graph on the right shows the quantification of this consistent blocking effect. This demonstrated the high affinity of the lanthanum-133 PSMA I&T for the LNCaP cells.
All of this data for our improved targetry, chemical separation, phantom and animal imaging was published in a recent article in the Journal of Nuclear Medicine.

## Slide 19: 203Pb Production Cross Sections of Interest
Cross section simulation data from TENDL 2019 (Koning et al.)

## Slide 20: New Target Assembly
Images credit of Advanced Cyclotron Systems Inc.
Switch from TA-1186 target assembly with direct water cooling to TA-2150-B target assembly with copper cold finger
Disc installed in target assembly, pressed onto copper cold finger with springs and air pressure
No cooling water activation with TA-2150-B
Slot for target loading
Cu cold finger
Notes: Adjusting the nuclear cross sections for this enriched isotopic abundance, we get two distinct reactions. Irradiating at a lower energy of 11.9 MeV allows high yield production of highly pure lanthanum-135 via the barium-135 p,n reaction, while irradiating at higher energies allows significant production of lanthanum-133 via the barium-135 p,3n reaction with lower amounts of co-produced La-135.

## Slide 21: Lead-203 Production
203Pb (t1/2 = 51.9 h, 279 keV (81%)) attractive radionuclide to provide theranostic SPECT imaging alongside 212Pb targeted radionuclide therapy
Thallium metal highly toxic and poor thermal conductivity (46 W⋅m-1⋅K-1)
Utilize sealed solid target assembly to encapsulate thallium metal target material
Bombard at 24 MeV (extracted), 23.3 MeV incident on 205Tl metal (99.9% enrichment) at 60 μA proton beam current
Water cooled by TA-2150-B copper cold finger on back, helium cooling on front

## Slide 22: Beam Distribution Optimization and Analysis
Investigate target thermal performance
Irradiate Cu discs at 60 μA for 1 min with beam tune for 18F liquid target (80% beam transmission) and beam tune optimized for 205Tl sealed solid target (55% beam transmission)
Expose irradiated targets to Gafchromic EBT film to investigate beam spread, digitize with a scanner for analysis
Image analysis performed using ImageJ
80% current transmission
55% current transmission
Max beam intensity
Min beam intensity
Melted thallium, Reduced 203Pb yield (<50% theoretical)
203Pb yield >90% of theoretical
1 cm
1 cm
1 cm
80% current transmission
55% current transmission
1 cm
Notes: Adjusting the nuclear cross sections for this enriched isotopic abundance, we get two distinct reactions. Irradiating at a lower energy of 11.9 MeV allows high yield production of highly pure lanthanum-135 via the barium-135 p,n reaction, while irradiating at higher energies allows significant production of lanthanum-133 via the barium-135 p,3n reaction with lower amounts of co-produced La-135.

## Slide 23: 203Pb Purification and Radiolabeling
203Pb saturated yield of 3.9 ± 0.3 GBq/μA
Tl/Pb chemical separation performed with Pb resin >12 hours after EOB (allows 204mPb decay)
Elute with 8M HCl, >85% decay-corrected [203Pb]PbCl2 yield in 4 mL
Can convert to [203Pb]Pb(OAc)2 with 1M NH4OAc elution using a second Pb resin
Maximum purified yield of 12 GBq [203Pb]PbCl2 (15.8 GBq at EOB) with 8.6 h irradiation, radionuclidic purity >99.9%
Radiolabeling [203Pb]Pb(OAc)2 with bifunctional chelators: 461  30 GBq/μmol with PSC-Bn-NCS, 195  37 GBq/μmol with TCMC-NCS, 83  16 GBq/μmol with DOTA-NCS
203Pb
HPGe gamma emission spectrum of [203Pb]PbCl2 product
PSC-Bn-NCS provided by Viewpoint Molecular Targeting
Separation modified from McNeil et al., EJNMMI Radiopharm Chem. 2021;6(1):6
Notes: Adjusting the nuclear cross sections for this enriched isotopic abundance, we get two distinct reactions. Irradiating at a lower energy of 11.9 MeV allows high yield production of highly pure lanthanum-135 via the barium-135 p,n reaction, while irradiating at higher energies allows significant production of lanthanum-133 via the barium-135 p,3n reaction with lower amounts of co-produced La-135.

## Slide 24: Summary
Nuclear reaction | Target material and mass | Target pellet incident energy (MeV) | Proton beam current (μA) | Saturated yield
135Ba(p,3n)133La | natBa metal, 200 mg | 23.3 | 10 | 277 MBq/μA
135Ba(p,n)135La | natBa metal, 150 mg | 11.9 | 10 | 167 MBq/μA
135Ba(p,3n)133La | natBaCO3, 200 mg | 23.3 | 10 | 204 MBq/μA
135Ba(p,n)135La | natBaCO3, 150 mg | 11.9 | 10 | 115 MBq/μA
135Ba(p,3n)133La | 135BaCO3 (92.7%), 200 mg | 23.3 | 10 | 736 MBq/μA
135Ba(p,n)135La | 135BaCO3 (92.7%), 150 mg | 11.9 | 10 | 1377 MBq/μA
68Zn(p,αn)64Cu | 68Zn metal (98.3%), 100 mg | 23 | 70 | 348 MBq/μA
68Zn(p,n)68Ga | 68Zn metal (98.3%), 100 mg | 12.5 | 10 | 5.6 GBq/μA
205Tl(p,3n)203Pb | 205Tl metal (99.9%), 250 mg | 23.3 | 60 | 3.9 GBq/μA
89Y(p,n)89Zr | natY metal, 150 mg | 13 | 10 | 4.6 GBq/µA

## Slide 25: Conclusions
Novel indium-aluminum sealed cyclotron target is robust, simple to manufacture, contains reusable components
Target assembly can be irradiated at beam currents up to 70 μA with no signs of degradation and minimal component activation
Target backing can be used as an intrinsic degrader
Easily adaptable to produce clinically relevant activities of various diagnostic or therapeutic radiometals with sensitive or hazardous target materials
Chemically compatible with multiple separation processes demanding high radiochemical purity

## Slide 26: Acknowledgments
Medical Isotope and Cyclotron Facility
Cross Cancer Institute
Dr. Frank Wuest
Dr. Jan Andersson
Dr. John Wilson
Dr. Melinda Wuest
Dr. John Duke
Dr. Hans-Sönke Jans
Dr. Susan Pike
Dr. Simon Ferguson
Dr. Jonathan Doupe
Cody Bergman
Blake Lazurko
Curtis Osinchuk
Steffen Happel (Triskem)
Jayden Sader (ACSI)
Notes: Finally, I’d like to thank my supervisors Dr. Frank Wuest and Dr. Jan Andersson and members of my supervisory committee for their support and guidance, the entire Wuest lab, and others from the University of Alberta and Alberta Health services working at the Cross Cancer and Medical Isotope and Cyclotron Facility whose expertise were invaluable for this project.