## Slide 1: SRF Development at TRIUMF
Philipp Kolb
RF/SRF Group
Science Week, Jul. 31, 2023

## Slide 2
Outline
SRF Overview
  ISAC-II
  ARIEL eLINAC
Research
  Coax. Cavities
  SRF Materials
SRF collaborations
  VECC
  Hi-Lumi LHC Crab Cavity Module
Future
  ISAC-II: Beyond 40MV
  eLINAC: reliable 30MeV
  EIC Crab Cavity

## Slide 3
RF Systems
ISAC-II
e-Linac
30MV 1.3GHz electron Linac
ISAC-I
Cyclotron
Medical Cyclotrons
40MV Heavy Ion Linac

## Slide 4
ISAC-II Superconducting Linac
40MV SC Linac with 40 106/141MHz Quarter-Wave Resonators (QWRs), operating at 4.2K
To accelerate Radioactive Ion Beams (RIB)
Each cavity provides ~1MV of accelerating voltage
In operation since 2006 – first 20 cavities
Full 40 cavities installed in 2010
~2300 hrs / year operation
Ongoing upgrade/maintenance program to maintain reliability
141MHz QWR
SCC3 Cryomodule
~1m
~20cm

## Slide 5
ARIEL e-Linac
30MV 1.3GHz electron Linac
Based on 1.3GHz technology used in XFEL / LCLS-II / ILC
Driver Linac for photo-fission to produce RIB
Operation at 2K
3 cavities, each providing 10MV
High beam power – currently up to 10kW but capable of more
Transitioning currently from Commissioning to Operation
1.3GHz elliptical 9cell cavity

## Slide 6
Research & Student Programs
Using the strengths and unique capabilities of TRIUMF to fill research voids and covering niche research topics with high impact
Coaxial cavities studies
Material science for next generation of SRF materials

## Slide 7
Coaxial Cavity Program
217MHz
648MHz
389MHz
778MHz
1166MHz
Multi-mode cavities allow frequency resolved measurement of cavity performance without changing cavities
Exploring how surface treatments impact performance – informs ISAC-II cavity retreatment, but also fundamental SRF interest
Niche, but important research for SRF community
* Follow-up paper in peer review

## Slide 8
SRF MSc Student Projects
Magnetic Flux Expulsion Studies on Coaxial Resonators
Ruth Gregory (MSc, UVic)
Modelling thermal feedback in surface resistance studies on coaxial SRF cavities
Mattias McMullin (MSc, UVic)
The rf surface resistance is highly dependent on the surface temperature
Question: How can we determine the RF surface temperature compared to the bath temperature?
External magnetic flux can negatively impact cavity performance.
Question: How does cavity shape, cavity frequency, field direction and cooldown speed impact flux trapping and performance?
Poster available during the poster session on Wednesday! Please come talk to Ruth there.
New data + model eliminates discontinuity when cooling regime changes.
Recognized at SRF 2023 conf with Student Poster Award (1st place)

## Slide 9
New `-SRF’ Facility Commissioned
at -NMR
Helmholtz coil
First paper
E. Thoeng, et al:
A New High Parallel-Field Spectrometer at TRIUMF’s 𝛽-NMR Facility,
Rev. Sci. Instr. *Editors Pick*
Edward was recognized at SRF2023 with the Early Career Presenter Award.
New beamline extension installed at -NMR facility for SRF materials characterization
Unique facility in the world for depth profiling materials in parallel magnetic fields up to 200mT – SRF regime – critical field of Nb
Collaboration between Accelerator Division and CMMS
Commissioning and first experiments completed
Edward Thoeng
(PhD, UBC)
Magnetic field screening for
various applied fields

## Slide 10
SRF Collaborations
Supporting the SRF community and engaging in cutting edge projects
VECC cryomodules
CERN Hi-Lumi crab cavity modules

## Slide 11
VECC Cryomodules, India
1.3 GHz Injector Cryomodule
Quarter-wave Resonator Heavy Ion Cryomodule
TRIUMF and VECC (Kolkata) have had an active collaboration since 2008
As part of the collaboration TRIUMF has completed two cryomodules, a 1.3GHz electron SRF module (ICM) and a 110MHz heavy ion module (QWR)
The ICM was shipped in 2019 and the QWR will be shipped in December 2022
TRIUMF is also completing RIB production modules for VECC

## Slide 12
CERN Hi-Lumi LHC Upgrade
4K/2K unit
RFD cryomodule
String assembly cart
Cavity handling
TRIUMF was funded to produce and qualify 5 RF Dipole (RFD) cryomodules as in-kind contribution
Preparing to build prototype cryomodule (TCM0) and to receive first cavities in 2023
Procurement is in progress.
Series production CMs will follow in 2024 and 2025
Also Beam Physics collaboration – Hui Wen in next talk for more details

## Slide 13
Outlook into the Future
ISAC-II: Beyond 40MV
eLinac: Reliable 30MeV operation
Electron-Ion Collider Crab Cavity

## Slide 14
Chart: Eacc [MV/m]
| 1.8633175492499654 | 2.4991186430447345 | 3.1425838499474645 | 3.7782167955949015 | 4.4237122979515604 | 5.0674196865352821 | 5.7185625300032692 | 6.0504388260512023 | 6.4089498654520396
SCC1#1 | 946856717.5213 | 776136995.4104 | 672968425.0309 | 586884389.2416 | 509931844.1431 | 423415729.3925 | 350616038.3217 | 308869220.5645 | 272909821.6997
SCC1#2 | 883659519.876 | 762848241.8366 | 666349979.9835 | 577824397.4794 | 473423573.4545 | 415705083.3761 | 352025296.2383 | 287507071.5743 | 224316023.5727
SCC1#4 | 868521721.9739 | 717820733.5601 | 625947431.6552 | 516997064.726 | 441220137.0782 | 358833217.3509 | 314898789.6708 | 273102233.5017 | 225402365.3979
SCC1#5 | 2082398964.9559 | 1945472505.0584 | 1869708060.0425 | 1729913024.8878 | 1543539860.3997 | 1389344025.6332 | 1250430337.3143 | 1122415249.3114 | 1004973227.3203 | 850129468.1692 | 699852842.8373 | 557157703.0094
SCC1#6 | 906982575.3671 | 704564359.4024 | 551695148.0776 | 391810923.5836 | 289080899.6439 | 186195964.6402
Q at 7W | 8479600.2086 | 33918400.8343 | 76316401.8771 | 135673603.3371 | 211990005.2143 | 305265607.5086 | 415500410.22 | 542694413.3486 | 686847616.8943 | 847960020.8571 | 1026031625.2371 | 1221062430.0343
ISAC-II: Beyond 40MV – Increasing Q0 & Eacc
Cavity performance characterized in quality factor and gradient
  SCC1#5 was used for R&D, resulting in much higher performance
Increasing cavity performance via different processes:
  Informed by coax cavity R&D
  Degassing in UHV at ~650-800C for hydrogen removal (~$500k for furnace)
  Low temperature bake (120C for 48hrs)
Higher higher Energy
Higher more cryogenic margin for more cavities!
Performance of SCC1 cavities
7W of cavity wall losses = cryogenic losses
Typical operating curve for ISAC-II
SCC1#5

## Slide 15
eLINAC: Reliable 30MeV Operation
Stable 30MeV operation is critical for RIB production:
RIB yield is strongly dependent on beam energy
We’re operating at 30MeV – at the lower end of the yield curve
Field emissions from contaminants in the SRF cavity limit RF performance to lower
Prevention and mitigation critical to keeping performance high, to keep RIB yield high
Field Emission limits performance to
Clean cavity reaches

## Slide 16
Development: Plasma Processing
Daniel Hedji (MSc – Uvic)
Plasma processing with an Ar/O mixture can break up hydro-carbon based particulates and remove them.
Would allow cavity cleaning without taking module off beamline (1 week instead of 2-3 months of work)
First Plasma ignition in a single cell cavity at TRIUMF.
Results from JLab show decreased FE after plasma processing

## Slide 17
Study: Field Emission and Dust migration
Aveen Mahon (MSc - Uvic)
To prevent particulate migration, we need to know how they move
Collaboration with CERN at the LHC and the University of Boulder, CO, to study the field emission and dust migration
Samples are placed inside beamline near SRF accelerators and collected periodically to characterize the particulates

## Slide 18
Electron-Ion Collider
A major new collider facility scheduled to be built at BNL to explore subatomic physics.
TRIUMF working with EIC-Canada to seek Canadian funding to support in-kind contributions.
TRIUMFs SRF group started work on the design of the 394MHz crab cavity – similar size to HL-LHC 400MHz crab cavity
Challenging HOM design due to high beam current
540mm
360mm

## Slide 19
Summary
Supporting SRF accelerators
  ISAC-II
  ARIEL eLINAC
Training students and Post-Docs
  Research program on Coax Cavities
  SRF material science at NMR
Contributing to SRF community
  VECC
  HL-LHC
  EIC

## Slide 20: Thank you Merci

## Slide 21
Beyond 40MV – more SRF
RFQ
SCA
18m
Low energy area
3 simultaneous RIBs to experiments
New RFQ to 400keV/u for A/q<7
SCA w/ 7 QWRs @ 71MHz, β 4.1%
Booster
to LE area
to ME area
to HE area
Increase RIB energy
Booster w/ 8 QWRs @ 141MHz, β 16%
Adding 16MV